## Slide 1
部件基本信息-General Part Information
39.7mm
218mm
354mm
Mold: | CH184-06A-DOWN
Part No: | 
No.of Cavity | 1*1
Mold Life(Shot) | 50K
Resin Material: | ADC12
Shrinkage Used: | 1.005
Material Density: | 2.7g/cm³
Part Volume: | 188.32/cm³
Part Weight: | 504g
Runner Weight: | 
Main Steel Insert: | 8407
General Hardness: | HRC47~48°
Mold Base Material | S50C
Runner (Cold/Hot) | 
Mold Type: | 2-Plate
Estimate Mold Size | 620/650/320
Estimate M/C Tonnage | 350T
Cosmetic requirements | 

## Slide 2
分型线-Define Parting Line (Cavity / Core Surface)
母模(CAVITY)
公模（CORE）
PL
分型线上的段差量和方向必须表达清楚。

## Slide 3
排位和浇口类型-Layout and Gating Type
浇口、流道、溢流块如图上图所示；溢流块数量：20
天侧

## Slide 4
模流分析-Mold flow analysis
通过分析未见明显卷气现象，略微不良 可通过后续增加排气或调机解决

## Slide 5
镶件线-Split line of Insert

## Slide 6
顶针位置和类型-PIN location and type
顶针位置图
圆顶针

## Slide 7
模具冷却水路-Tooling Cooling System proposal
Cav. Cooling System
Core Cooling System

## Slide 8
拔模角度/表面处理/外观要求-Draft Angle / Surface Finishing / Cosmetic Concern or Requirement

## Slide 9
此处三个绿色面没有设计脱模斜度，建议修改到单边1.5度。
改善和建议-Proposal for structure

## Slide 10
靠进料一侧建议壁厚加厚到2.0以上，保证进料口有平位，剩下的地方圆弧过度接顺。
改善和建议-Proposal for structure

## Slide 11
5支头部2.6的镶针需多做备用针。
改善和建议-Proposal for structure